Adhesion promoter

ADP

**Features and advantages:**

1. Excellent adhesion to aluminum alloy, zinc plate, stainless steel, electroplating surface, iron and other metal surface.

2. High temperature baking paint does not change color, and does not affect other properties.

3. It can improve the toughness and impact resistance of the film.

4. Does not affect the storage stability of coating, high temperature resistance of more than 280℃.

**Product specifications:**

|  |  |
| --- | --- |
| appearance | Pale yellow liquid |
| composition | Polymer surface adjuster solution |
| Valid copy of | 70% |
| solvent | N-butyl alcohol |

**Application:** metal paint, aluminum, zinc, stainless steel, aluminum alloy surface treatment.

**Recommended dosage:** 1 -- 5% of total formula (please test the most appropriate dosage before use)

**Directions:** Add to top coat and mix well.

**Packaging:** 25KG non-recycled blue plastic bucket; Before the product is fully used, the lid should be tightly closed after use.

**Storage:** keep away from heat and fire and keep away from light.